SiON channel waveguides for sensor applications

P. L. Pernas*, E. Ruiz, J. Piqueras

# Departamento de Física Aplicada CXII, Universidad Autónoma de Madrid, 28049 Madrid, Spain

F. Paszti, A. Climent-Font

Centro para el Microanálisis de Materiales, Departamento de Física Aplicada CXII, Universidad Autónoma de Madrid, 28049 Madrid, Spain

(b)

(a)

E. Cantelar, F. Cussó, G. Lifante

Departamento de Física Materiales CIV,

Universidad Autónoma de Madrid, 28049 Madrid, Spain

Contacto: (*) Tel.: 913978560, Fax: 913973969 e-mail: pablo.pernas@uam.es

Areas de Interes: Integrated optics, Sensors Palabras Clave: Waveguides, RBS, ERDA, SiON, Sensors

### 1.- Introduction

Sensors are in great demand by industry for a wide range of situations as control and detection of vapors in environments, biotechnology, etc.. Many characteristics of the light are suitable to carry the sensor information: the intensity, the phase, the direction, the polarization and the wavelength. Also exist many useful optical cross-effects that can produce the transduction function of the sensing action as electro-optic, thermo-optic, mechano-optic, or chemo-optic effects. In this optical scenario it is naturally preferred to incorporate these opto-sensing mechanisms in a guided configuration either in fiber or on a waveguide. The central idea of this paper is to develop microelectronic semiconductor technologies in order to obtain integrated optical sensors [1,2].

2.- Technology

Silicon-based thin films on silicon substrates are very promising materials for the fabrication of passive or active channel waveguides for low-cost integrated optics (IO) since they are compatible with silica fibers used in telecommunications and enables hybrid or monolithic integration with active optoelectronic devices. Among the more interesting optical materials is the SiON. The SiON has several features that could let it play an important role in IO. The advantages are SiON's high index of refraction and low loss characteristics allow designers to fabricate small, highly complex functions on surfaces. Scientists have developed waveguides made of SiON between two layers of silicon dioxide using standard microelectronic methods. The two materials show a high contrast of the refractive index, i.e. a light is confined strongly to the SiON waveguide and the refractive index can be varied by changing the content of H [3,4].

Fig.1. (a) Photograph of the six channel waveguides on Si3N4 material fabricated with ECR and RIE without the final cladding of SiO2. (b) SEM image of the cleaved edge of the waveguide.

In telecom technology, the impulse response of a waveguide, and consequently the information-carrying capacity, is dependent on these parameters. So, it is essential to produce particular and controlled waveguide index profiles with great accuracy. Controlling the precursor gases in the deposition chamber, the nitrogen-to-oxygen relation in SiON material can be chosen freely. This allows the refraction index of the waveguide to be adjusted from the SiO2 index, nSiO2 = 1.47 to the pure Si3N4, nSiN = 2.00. In particular ECR plasma deposition method implies low temperatures at high deposition rates, a great homogeneity  across the whole wafer extension with a very low final damage. Unfortunately films deposited using silane (SiH4), as the silicon precursor, and ammonia (NH3) or deuteroammonia (ND3) as nitrogen precursor, suffer from two high absorption in the most interesting wavelength range for optical communication 1,3 to 1,55 microns [5,6]. These films contains high concentration of bonded hydrogen in form of Si-H, O-H and N-H. bonds, that are responsible of such infrared absorption [7]. In order to reduce the H content, we have improved the ECR deposition process using N2 as nitrogen precursor.

### 3.- Experimental

The initial stage of the dielectric waveguide fabrication starts with the careful cleaning of standard Si wafers that were covered with 1.5 m of thermal oxide. The following layers are deposited  by means of the ECR. The SiO2 cladding is deposited from 5% Ar diluted SiH4, N2 and O2 as precursor gases. The high maximum index contrast between core and cladding films is obtained for a pure SiN material, where nSiO2 = 1.46 and nSiN = 2.02. To define the strips on core film, UV-photolithographic techniques were used. In the case of SiN waveguides, a cladding thickness of tSiO2 = 0.5 m and a core thickness of tSiN = 0.5 m have been proved adequate to avoid wave propagation of the fundamental mode into the Si wafer. The final structure before the over-cladding process is shown in the optical microscope photograph presented in figure 1. The characterization of the plane waveguides has been performed by m-line spectroscopy at 633 nm. In the case of the waveguide of Si3N4 core, we have observed two modes (both TE and TM). In figure 2 we show the real output optical modes of the channel waveguide, recorded with a HeNe laser (633 nm) and a CCD camera.

Fig.2 Output modes of the SiN channel waveguide recorded with a HeNe laser (633 nm) and a CCD camera.

The composition of SiN samples was determined by ion beam analysis using the new installed HVEE 5 MV tandem accelerator from HVEE in the Center for Micro-Analysis of Materials at Universidad Autónoma of Madrid. Rutherford backscattering spectrometry (RBS) with a beam of 2 MeV He ions detected at 171º was used to find out the relative amount of Si and N in the films. The content of H, and also N, in the film was determined by elastic recoil detection analysis (ERDA) using a 29 MeV Si beam as the incident ions. The recoils of H and N were detected at an scattering angle of 34º tilting de sample 73º towards the detector. The appearance of the signal from N in both types of spectra; RBS and ERDA, is used as a reference that allows easily to determine the relative amount of the three elements in the film, H, N, and Si, in a precision of about 5 %. The thickness of the film can also be obtained with a similar incertitude.

Fig 3a and Fig 3b show, respectively, the RBS and ERDA spectra of SiN sample not subjected to heat treatment. In the RBS spectrum the element Si in the SiN film is observed between channels 310 and 340 approximately.

(a)

(b)

Fig. 3. (a) RBS spectrum of 2 Mev He ions backscattered from SiN sample. Scattering angle 171º. The modelling has been performed assuming an areal density of 450 x 1015 atoms/cm2 with  a molar composition of 0.35 of Si, 0.58 of N 0.06 of H and 0.01 of  O. (b) ERDA spectrum of 29.3 Mev Si ions. The scattering angle was 34º. We can observe the hydrogen peak (channel 750) and a wider peak of nitrogen.  The continuous line shows the modelization, assuming the same thickness and composition as in RBS simulation.

The edge at channel 340 is the Si surface signal, that is the signal generated from the Si atoms at the surface of the sample. As the collisions occur deeper in the sample the backscattered He atoms escape from the sample with less energy, and, consequently, they are detected at lower channels. In channel 310 we observe the interface of the SiN film with the substrate. The increase in yield now observed indicates that we have reached the substrate with a higher concentration of Si atoms. Going still towards lower channel number we observe at channel 175 the surface signal from the O overlapped with signal from Si atoms from the substrate. For a given scattering angle, the backscattered particle has less energy as the mass of the scattering center decreases. Around channel 155 it is the signal from the O at the interface of the film with the Si substrate.

In RBS only He is detected, while that in ERDA the recoiled atoms from the sample are detected. In Fig 3b we can see then the detected N atoms as the signal between channels 600 and 1200, and the H signal is the sharp peak centered in channel 750. Although the H is located more or less uniformly across the SiN film, its signal appears narrower because it has a lower stopping force than the N.

As the processes involved in the MeV elastic atomic collisions and energy loss are very well known, computer codes exist that can synthesize RBS and ERDA spectra. The precise composition of the sample is obtained comparing a simulated spectrum with the experimental one. The simulation is generated feeding to the program an assumed composition and thickness of the samples, as well as the experimental parameters like kind and energy of the beam, geometrical disposition of the detectors, etc. In both types of spectra, RBS and ERDA, the same composition for the sample was assumed, and the results are shown as continuous line in Fig 3a and 3b [8].

In the case of SiON, in order to change the refraction index and simultaneously to reduce losses, we have used N2 as precursor gas to control the nitrogen-to-oxygen relation present in SiON samples. In this manner we have fabricated and characterized monomode waveguides with index of nSiON = 1.540 and 1.665 that contains a lower quantity of H than in alternative methods [4]. Results of m-line spectroscopy are presented in figure 4. The optical losses at 633 nm were inferred from this modelization by considering the relative scattered light into the substrate. For the fundamental mode (Mode 0) a maximum optical loss of 0.8 dB/cm has been determined. Further RBS and ERDA composition studies of SiON samples are in progress.

- Fig. 4. Simulated intensity and refractive index profiles with experimental m-line data. The (structural) scattering losses of the mode 0 were 0.8 dB/cm. (nSiON = 1.530 sample)

- 4.- Conclusions

- In summary a fabrication method of channel buried waveguides has been developed. SiN and SiON ECR films are deposited and etched at very low temperatures in short times with a low surface damage. Never during the fabrication steps were the samples submitted to temperature above 100ºC. The SiON refractive index can be varied by changing N2 precursor flux during the deposition. RBS and ERDA composition measurements are presented. Dielectric waveguides presented here show clearly that this technique is a promising and versatile method for fabrication of low cost waveguides compatible with fibers that can be monolithically integrated with active devices in opto-sensors devices.

5.- References:

[1] R. G. Heideman, G. J. Veldhuis, E. W. H. Jager, and P. V. Lambeck, Sensors and Actuators B: Chemical, 35, 234-240, 1996.

[2] P. L. Pernas, M. J. Hernández, E. Ruíz, E. Cantelar, R. Nevado, C. Morant, G. Lifante and F. Cussó, Applied Surface Science, 161, 1-2, 123-130, 2000.

[3] R. Germann, H.W.M. Salemink, R. Beyeler, G.-L. Bona, F. Horst, I. Massarek and B.J. Offrein, in “Silicon Nitride and Silicon Dioxide Thin Insulating Films”, ed. by K.B. Sundaram, M.J. Deen, W.D. Brown, R.E.Sah, E. Poindexter, D. Misra, The Electrochemical Society, Pennington, 99, 169-181, 1999.

[4] M. Hoffmann, P. Kopka and Edgar Voges, IEEE Photonic Technol. Lett., 9, 9, 1238-1240, September 1997.

[5] D. E. Kotecki and J. D. Chapple-Sokol, Journal of Applied Physics, 77, 3 1284-1293, 1995.

[6] T. P. Smirnova L. V. Yakovkina, Thin Solid Films 293, 6-10, 1997.

[7] A. Benmessaoud, A. Llobera, M. Riera, N. Mestres, J. Pascual, C. Dominguez, J. A. Rodríguez, 2nd Spanish Conference on Optoelectronics, OPTOEL01, Barcelona, Spain, July 2001.

[8] M. Mayer, SIMNRA User's Guide, report IPP 9/113, Max-Plank-Institute (1997).

This work was supported by MCyT projects TIC-2002-00147 and CF08-541A-A-640.